# SECTION 10 11 00

# VISUAL DISPLAY BOARDS

# PART 1- GENERAL

# 1.1		SUMMARY

A.	Section Includes:

1.	Dry-erase Markerboards (Single Track Marker Boards) (Double Track Wallboards) (Flexible Component Boards)

2.	Chalkboards (Single Track Chalkboards) (Double Track Chalkboards) (Flexible Component Boards)

3.	Tackboards (Noticeboards) (Flexible Component Boards)

4.	Combination Boards (Combi Boards)

3.	Systems/Presentation Rails (Single Track Rail) (Double Track Rail) (Sliding Rail System with Pen shelf/Marker-Chalk Tray)

B.	Related Sections:

1.	Section 06 10 00 – Rough Carpentry: Wood blocking

2.	Section 09 29 00 – Gypsum Board

3.	Section 09 72 00 – Wall Coverings

4.	Section 09 91 00 – Painting

# 1.2		SUBMITTALS

A.	Product Data: Provide technical data for products specified.

B.	Shop Drawings: Provide shop drawings for each type of visual display board specified, including section details indicating trim, face, core and backing materials, wall elevations, dimensions, joint locations between panels exceeding maximum panel length and anchor and installation details

C.	Product Samples: Submit manufacturer’s color chart showing the full range of colors available for the following:

1.	Chalkboards and Markerboards: Actual sections of porcelain enamel steel finish for each type of chalkboard and whiteboard required

2	Aluminum Trim and Accessories: Samples of each type and color, on 6-inch (150mm) long sections of extrusions and not less than 4-inch (100mm) squares of sheet or plate. Include sample sets showing the full range of color variations expected

D.	Contract Closeout Submittals:

1.	Maintenance Data: Manufacturer’s cleaning and maintenance instructions covering both routine (daily or weekly) and long term (yearly or longer) operations

2.	Warranty: Executed copy of manufacturer’s warranty

# 1.3		DELIVERY, STORAGE AND HANDLING

A.	Storage and Protection:

1.	Store factory framed units vertically with packaging materials between each unit to prevent damage

2.	Store materials in dry areas at temperatures above 55º F

# 1.4		PROJECT CONDITIONS

A.	Field Measurements: Verify field measurements before fabrication to ensure proper fitting.  Coordinate fabrication schedule with construction progress to avoid delaying the work. Notify the Architect of any conflicts with other construction such as casework, electrical switches, outlets, clocks, mechanical openings, fire detector devices, etc

B.	Environmental Requirements: Install only when the building is enclosed and interior air and substrate temperatures are stable and approximate design conditions

# 1.5		WARRANTY

A.	Porcelain Enamel Writing Surface Warranty: Submit a written warranty executed by the manufacturer agreeing to replace porcelain enamel steel markerboards/chalkboards that do not retain their original writing and erasing qualities, become slick and shiny (if matt surface), or exhibit crazing, cracking or flaking within the specified warranty period, provided the manufacturer’s written instructions for handling, installation, protection and maintenance have been followed

1.	Warranty Period: Forever Warranty on CPS Porcelain Markerboards and Chalkboards

B.	Noticeboard, Combination Board, Flexible Component Board, and VIP Rail Warranty: Submit a written warranty executed by the manufacturer agreeing to replace Noticeboards, Combination Boards, Flexible Component Boards, and VIP Rail that exhibit manufacturer defect within the specified warranty period, provided the manufacturer’s written instructions for handling, installation, protection, and maintenance have been followed.

- Warranty Period: Minimum (2) years from date of completion

# PART 2- PRODUCTS

2.1		MANUFACTURERS

A.	Basis-of-Design Product: Corona Group VIP Series Visual Presentation  Products - Dry-erase Markerboards, Chalkboards, Noticeboards, Combination Boards and VIP Rail are based on Corona Group VIP  Series: Contact info@coronagroupinc.com or call 205-941-1942 – www.coronagroupinc.com

B.	Approved Alternates: (Due to the unique nature of the Corona system, please contact Corona Group for specific information regarding alternative products)

C.	Additional alternates must have prior approval.  Submit technical information and samples to architect a minimum of 14 days prior to bid date

2.2		MARKERBOARDS

A.	VIP SERIES Single Track Markerboards and Double Track Wallboards: Magnetic Dry-erase markerboards for marker pens and magnets

1.	Finished Surface: CPS Satin Gloss, scratch-resistant, porcelain enamel steel .4 - .6mm thick; fused twice between 1200º - 1600º F

2.	Core/ Substrate:

a. 	7/16” Medium Density Fiberboard (MDF) laminated to face steel for single piece boards up to 16’

3.	Backing: Foil, laminated to core/substrate

4.	Sizes: As indicated in Drawings

5.	Frame Profile: Manufacturer’s standard

6.	Top and Bottom Frames: Natural anodized extruded aluminum, 2mm thick, and 60mm high x 20mm/40mm deep.  Rail shall be slotted to accept concealed mounting hardware and ship complete with mounting sets

7.	Sliding Tracks (integral and concealed) for hanging flexible boards; flip charts projection boards, noticeboards, chalkboards, glassboards and additional whiteboards consistent with VIP Series Design and Specifications

a.	Top frame for Single Track Whiteboards shall have one (1) sliding track

b.	Top frame for Double Track Wallboards shall have two (2) sliding tracks

c.	Top frame for Double Track Wallboards shall have a concealed chamber to house ball bearings suitable for displaying paper from the top rail

8.	Side Profiles: Natural anodized extruded aluminum 2mm thick, 6mm wide x 20mm deep

9.	Accessories:

a.	Provide one accessory pack for each marker/wallboard.  Accessory Pack shall include four (4) dry-erase markers, one (1) magnetic penholder, one (1) magnetic felt eraser, one (1) package of ten (10) replacement eraser pads, one (1) package of three (3) Eximo™ whiteboard cleaning pads and one (1) soft drying cloth and twelve (12) round Teflon coated magnets

10.	Board Color: Satin Gloss White unless otherwise specified

11.	Optional:  Full Length Aluminum Pen Shelf docks to bottom rail of whiteboard or wallboard. Or can be magnetic or wall mounted

2.3		CHALKBOARDS

A.	VIP SERIES Magnetic Chalkboards and Wallboards

1.	Finished Surface: CPS Matt, scratch-resistant, porcelain enamel steel .4 - .6mm thick; fused twice between 1200º - 1600º F

2.	Core/Substrate:

a. 	7/16” Medium Density Fiberboard (MDF) laminated to face steel for single piece boards up to 16’

3.	Backing: Aluminum foil, laminated to core

4.	Sizes: As indicated on Drawings

5.	Frame Profile: Manufacturer’s standard as specified

6.	Top and Bottom Frames: Natural anodized extruded aluminum, 2mm thick, and 60mm high x 20 mm /40 mm deep.  Rail shall be slotted to accept concealed mounting hardware and ship complete with mounting sets

7.	Sliding Tracks (integral and concealed) for hanging flexible boards; flip charts, notice boards, markerboards, glass boards and additional chalkboards consistent with VIP Series Design and Specifications

a.	Top frame for chalkboards shall have one (1) sliding track

b.	Top frame for wallboards shall have two (2) sliding tracks

c.  	Top frame for wallboards shall have a concealed chamber to house ball bearings suitable for displaying paper from the top rail

8.	Side profiles: natural anodized extruded aluminum 2mm thick, 6mm wide x 20mm deep

9.	Accessories: Provide one accessory pack for each chalk/wall- board.  Accessory Pack shall include one (1) box of ten (10) sticks of white chalk, one (1) non-magnetic foam eraser and twelve (12) round Teflon coated magnets

10.	Board Color: Matt Black unless otherwise specified

11.	Optional:  Full Length Aluminum Pen Shelf docks to bottom rail of chalkboard or wallboard.  Or can be magnetic or wall mounted

2.3	MARKERBOARD/CHALKBOARD – FLEXIBLE BOARDS

A.	VIP SERIES Flexible Markerboard/Chalkboard: Magnetic Dry-erase markerboards for hanging on VIP single or double top rail

1.	Face Sheet: CPS Satin/Matt, scratch-resistant, porcelain enamel steel .4 - .6mm thick; fused twice between 1200º - 1600º F

2.	Core:

a.	19mm honeycomb core laminated to each face

3.	Frame Profile: Manufacturer’s standard

4.	Top and Bottom Frames: Natural anodized extruded aluminum, 2mm gauge, and 60mm high x 22.25 mm deep.  Frame shall be slotted to accept concealed machined corner brackets and hardware.  Boards ship complete with mounting sets for suspension in sliding tracks on single or double rails.

5.	Mounting Hardware: Supplied with standard narrow brackets for the single rail for bi-level presentation systems. Optional deep brackets available for tri-level presentation systems

6.	Factory assembled flexible noticeboards (fabric/cork/rubber/PET) to sizes indicated in drawings or specifications

7.	Side Profiles: Natural anodized extruded aluminum 2mm gauge, 6mm wide x 25mm deep

2.4	RAIL SYSTEM/PRESENTATION RAIL (PEN SHELF/MARKER-CHALK TRAY)

A.	Top and Bottom Rails: Natural anodized extruded aluminum, 2mm thick, and 60mm high x 20 mm /40 mm deep.  Rails shall have finished end caps of matching finish and height and depth dimension – 6mm wide. Rails and Trays available in custom lengths up to 16’ long in a single piece. Rail shall be slotted to accept concealed mounting hardware and ship complete with mounting sets

1.	Sliding Tracks in Top Rail (integral and concealed) for hanging flexible boards; flip charts, notice boards, markerboards, glass boards and additional chalkboards consistent with VIP Series Design and Specifications

a.	Single top rail shall have (1) sliding track

b.	Double top rail shall have (2) sliding tracks

c.	Single or double rail shall have a concealed chamber to house ball bearings suitable for displaying paper from the top rail

2	Bottom Rail

a.	Standard bottom rail shall have three sided face plate

b.	Pen shelf bottom rail shall have two sided face plate when used with pen shelf/marker-chalk tray or as presentation rail (Pen shelf integrates with the bottom rail same as with the standard board system)

B.  	Pen Shelf/Marker-Chalk Tray: Natural anodized extruded aluminum, 2mm thick, and 70mm high (rear) x 20 mm high (front) x 60mm deep.

a.	Pen shelf/marker-chalk tray may be installed without Bottom Rail using counter-sunk stainless screws for direct mounting to wall surface

2.5		FABRICATION

A.	Porcelain Enamel steel writing board facing sheet and foil backer

sheet shall be laminated to the to core material under pressure with manufacturer’s recommended flexible, waterproof adhesive

B.	Assembly: Provide factory-assembled writing board units, as required.  Writing boards to 16 feet should be factory framed in a single panel and delivered to the job site for installation using concealed fasteners.  Boards over 16 feet should be spliced and “field installed” directly to the wall using concealed fastening systems recommended by the manufacturer. Splices should be as follows:

1.	Make joints only where total length exceeds maximum length.  Fabricate minimum number of joints, balanced around center of board, coordinate with Architect for approval

a.  	One Piece length of Marker or Chalkboard – Maximum of 16’

b. 	One Piece length of Top and Bottom Rail (Frame) – Maximum 16’

c. 	One Piece length of Rail System/Presentation Rail (Marker-Chalk Tray) –’ Maximum 16’

2.	Provide manufacturer’s standard vertical butt joint system between abutting sections of writing boards accompanied by a spline of metal or wood to ensure proper alignment – Standard ¼” Side Profile per board

3.	Provide manufacturer’s standard mullion trim at joints between writing boards – Maximum 12mm (½”) wide H- Profile with finish to match frame

4.	Make available seamless concealed splicing kit of parts for field installation upon request

2.6		FINISHES

A.	Comply with NAAMM’s “Metal Finishes Manual for Architectural and Metal Products” for recommendations relative to applying and designating finishes

B.     	Manufacturer’s Standard finishes as designated above

# PART 3- EXECUTION

# 3.1		EXAMINATION

A.	Examine wall surfaces, with installer present, for compliance with requirements and other conditions affecting visual display board/rail installation

B.	Verify flat wall surfaces for proper board installation; provide concealed shims as necessary within Architect’s acceptable variance. Minimum Level 4 finished wall required by contractor.

C.	Do not proceed with installation until unsatisfactory conditions have been corrected

# 3.2		INSTALLATION

A.	Deliver factory built visual display boards/rails, completely assembled in one piece without joints, where possible.

B.	Install units in locations and mounting heights as indicated on drawings and according to manufacturer’s written instructions.  Keep perimeter lines straight, plumb and level. Provide grounds, clips, backing materials, adhesives, brackets, anchors, trim and accessories necessary for complete installation.

C.	Coordinate project site assembled units with grounds, trim and accessories. Join with a neat, precision fit.

# 3.3		CLEANING

A.	Clean units according to manufacturer’s written instructions.

B.	Cover surface of all units with protective cover taped to frame.

C.	Remove protective cover and tape on date of Substantial Completion.

# END OF SECTION

Rev. 02—02-2021